## Slide 1: Towards a Cheap and Environmentally Friendly Polymer Based Battery
Andreas Grasser, 13.12.2021

## Slide 2: Motivation
Large fluctuations in the production of renewable energy
 Need for the storage of large amounts of energy
Fraunhofer ISE (energy-charts.info)

## Slide 3: Motivation
Environmental and humanitarian issues of traditional Li-Ion batteries
Dangerous, flammable organic electrolytes
For stationary applications energy density is no big problem
Sodium-ion batteries
Cobalt Mine in the Congo

## Slide 4: Motivation
Electrodes | Electrolyte
Cheap | Cheap
Environmentally friendly | Safe
Good stability | Large stability window
… | …
+ current collectors

## Slide 5: Electrode

## Slide 6: Carbon Cloth Current Collectors
Flexible carbon-based current collector
Normally hydrophobic
After 2M H2NO3 treatment: hydrophilic
3D-printed holder with titanium contact
untreated
after treatment

## Slide 7: Polyaniline as Electrode Material
Cheap polymer
Environmentally friendly
Charge storage through adsorption
Emeraldine salt conductive  conductive coatings
Two redox peaks

## Slide 8: Polyaniline as Electrode Material
Preparation of the electrodes:
H2NO3-treated carbon cloth as substrate
Dropcasting 25µl of NMP-PANI onto the carbon cloth
 Mass loading: ~0.35mg
Drying at ~100°C

## Slide 9: Polyaniline as Electrode Material
Cheap polymer
Environmentally friendly
2 redox peaks
Better peak separation and higher capacity in HCl acid  Due to H+ adsorption or due to PANI salt state?
Vs. Ag/AgCl

## Slide 10: Polyaniline as Electrode Material
8M NaClO4
0.5M HCl
8M NaClO4
+ 0.5M HCl
(15:1)

## Slide 11: Electrolyte

## Slide 12: Stability Window of the Electrolyte
Aqueous electrolytes have a relatively low stability window

## Slide 13: Solid State (Polymer) Electrolytes
e.g. Polyvinyl Alcohol (PVA)
+ also acts as a separator
- poor conductivity

## Slide 14: Water Based Electrolytes
Concentrated aqueous electrolyte
Mixed organic-aqueous electrolytes
Hydrate melt
Gel Electrolyte

## Slide 15: Water Based Electrolytes
Concentrated aqueous electrolyte
Mixed organic-aqueous electrolytes
Hydrate melt
Gel Electrolyte
Yamada, Y., Usui, K., Sodeyama, K. et al. Hydrate-melt electrolytes for high-energy-density aqueous batteries.

## Slide 16: Water Based Electrolytes
Concentrated aqueous electrolyte
Mixed organic-aqueous electrolytes
Hydrate melt
Gel Electrolyte
N.R. Chodankar, D.P. Dubal,A.C. Lokhande, C.D. Lokhande,
Ionically Conducting PVA-LiClO4 Gel Electrolyte for High PerformanceFlexible Solid State Supercapacitors

## Slide 17: Water Based Electrolytes
Gel electrolytes are good candidates for cheap and safe batteries

## Slide 18: Gel Electrolyte using PVA
Good solubility in water
Cheap
Environmentally friendly

## Slide 19: Problem of Carbon Cloth Surface Oxides
Full CV over the whole stability window not possible due to surface oxides
Two half CVs over several cycles

## Slide 20: Problem of Carbon Cloth Surface Oxides
Full CV over the whole stability window not possible due to surface oxides
Two half CVs over several cycles
1st cycle
2nd cycle

## Slide 21: Gel Electrolyte using PVA
With low concentrations of PVA no larger stability window visible

## Slide 22: Gel Electrolyte using PVA
With low concentrations of PVA no larger stability window visible
No real gel electrolyte
Larger amount of PVA necessary

## Slide 23: Further Plans and Current Problems
For gel electrolyte: no Ag/AgCl-reference electrode possible
Oversized (NiHCF) counter electrode?
Compare different ways of PANI coating:
  Electropolymerisation of aniline (thin films)
  Slurry mixing (larger mass loading)