## Slide 1: Exploring the Feasibility to make a “Paint Battery”
Andreas Grasser, 26.06.2021

## Slide 2: Motivation
Battery production has many steps
In-situ production often impossible
More steps  more expensive
Reduction of production steps can lead to lower prices and broader applications

## Slide 3: Final goal
One paint that produces the three layers of a battery by itself:
  cathode
  gel electrolyte / seperator
  anode
“Wall paint that forms a battery”
https://www.obi.de

## Slide 4: Final goal

## Slide 5: Possible steps
Solvability experiments with the components
Simple phase separation experiments
Manually assembled battery using spin-coating etc. for benchmark
“Hybrid” battery with self-stratification of two layers + one spin-coated layer
Complete battery using self stratification
Further improvements
Reality: not that straight forward

## Slide 6: Final goal
Main material focus:
Polyaniline (PANI)
Polyethylene glycol (PEG)
Polyvinyl alcohol (PVA)
Alizarin
N-Methyl-2-pyrrolidone (NMP)
https://www.sigmaaldrich.com

## Slide 7: Polyaniline reduction / oxidation
Song, Edward & Choi, Jin-Woo. (2013). Conducting Polyaniline Nanowire and Its Applications in Chemiresistive Sensing. Nanomaterials. 3. 498-523. 10.3390/nano3030498.

## Slide 8: Solvability experiments
One solvent needed for all three polymers
Bottleneck in solvability: PANI
Experiment: PANI with different solvents and different treatments
→ NMP as a good candidate
Solvent has influence on stratification process
Also: PANI with shorter chain length better

## Slide 9: Manual Battery
Creating the layers of the battery without self-stratification
Using well-known techniques for battery fabrication
Benchmark for the final battery
Allows to move stepwise towards a complete self stratifying battery

## Slide 10: Manual Battery

## Slide 11: Manual Battery
Problem: Electropolymerisation of PANI on metal surfaces did not work
Can one dropcast PANI instead of electropolymerize it?
 CV of drop casted PANI (in 8M NaClO4)

## Slide 12: Manual Battery
Using DIY 3D-printed spin coater

## Slide 13: Contact angle measurements
Measure hydrophility of surface
→ possible test for a successful stratification
→ with different liquids: measurement of free surface energy possible
+ Very fast and easy
Many error sources
(soaking into PANI, dirt on surface, different film thickness, …)

## Slide 14: Contact angle measurements
Compare contact angle of different samples:
  Polyaniline
  PVA/PEG
  Polyaniline + PVA/PEG
For a successful stratification: contact angle of mixture should show strong tendency towards one of the single components

## Slide 15: Contact angle measurements

## Slide 16: The self-statification process
Driving forces for self-stratification:
  Gravity
  Selective wetting mechanism
  Pigment wetting mechanism
  Surface tension gradients
  Phase contraction
Two models for predicting self-stratification:
  UNIFAC model
  Surface energy based model

## Slide 17: The surface energy based model
Assumptions:
  Surface free energy is main driving force of stratification
  Solvent has no influence in stratification
+ Relatively easy to measure and calculate
- Even in an advanced form no perfect prediction possible

## Slide 18: The surface energy based model
3 conditions:
Christopher Carr, Eva Wallstöm, Theoretical aspects of self-stratification (1996)
https://doi.org/10.1016/0300-9440(95)00594-3

## Slide 19: The surface energy based model
Possibility to estimate interfacial surface tension from surface energies:
: dispersive component of surface free energy
: polar component of surface free energy

## Slide 20: Battery with two layer stratification
No stratification signs for PEG

## Slide 21: Battery with two layer stratification
Stratification of Polyaniline + PVA on Aluminum foil?

## Slide 22: Battery with two layer stratification
Big problem: how to add third layer beneath the coating?
Using a zinc surface as anode and Zinc Perchlorate as conducting salt
Difficulties (?):
  Zinc has different surface energy than Aluminum
  Zn2+ /Cl- instead of Na+ ions

## Slide 23: Battery with two layer stratification
First test with copper current collector gave a voltage of ~0.6V
(Reaction directly between zinc ions and copper foil?)

## Slide 24: Battery with two layer stratification
Next time in the lab: Using two zinc current collectors

## Slide 25: Manual zinc battery
PVA easily solvable in NMP
↯ Spincoating of PANI on top of PVA not possible
 Building the battery bottom up

## Slide 26: Ways to do three layer stratification
Try stratification by free surface energy mechanism
Not many three-layer stratifications reported in the literature
Complete & reliable stratification is necessary (short circuits!)
Using a magnetic third component to force stratification

## Slide 27: Further plan
Build a complete working manual zinc based battery
Determine the surface free energy of the coatings
Use elipsomerty to do advanced testing for self-stratification
…?