## Slide 1: Exploring the Feasibility to make a “Paint Battery”
Andreas Grasser, 26.07.2021

## Slide 2: Motivation
Battery production has many steps
In-situ production often impossible
More steps  more expensive
Reduction of production steps can lead to lower prices and broader applications

## Slide 3: Final goal
One paint that produces the three layers of a battery by itself:
  cathode
  gel electrolyte / seperator
  anode
“Wall paint that forms a battery”
https://www.obi.de

## Slide 4: Final goal

## Slide 5: Possible steps
Solvability experiments with the components
Simple phase separation experiments
Manually assembled battery using spin-coating etc. for benchmark
“Hybrid” battery with self-stratification of two layers + one spin-coated layer
Complete battery using self stratification
Further improvements
Reality: not that straight forward

## Slide 6: Polyaniline reduction / oxidation
Song, Edward & Choi, Jin-Woo. (2013). Conducting Polyaniline Nanowire and Its Applications in Chemiresistive Sensing. Nanomaterials. 3. 498-523. 10.3390/nano3030498.

## Slide 7: Contact angle measurements
Measure hydrophility of surface
→ possible test for a successful stratification
→ with different liquids: measurement of free surface energy possible
+ Very fast and easy
Many error sources
(soaking into PANI, dirt on surface, different film thickness, …)

## Slide 8: Contact angle measurements
Compare contact angle of different samples:
  Polyaniline
  PVA/PEG
  Polyaniline + PVA/PEG
For a successful stratification: contact angle of mixture should show strong tendency towards one of the single components

## Slide 9: Contact angle measurements

## Slide 10: Battery with two layer stratification
No stratification signs for PEG

## Slide 11: Battery with two layer stratification
Stratification of Polyaniline + PVA on Aluminum foil?

## Slide 12: Battery with two layer stratification
Big problem: how to add third layer beneath the coating to electrochemically test the coating?
?

## Slide 13: Battery with two layer stratification
 Using a zinc substrate as anode and Zinc Chloride as conducting salt
Possible difficulties:
  Zinc has different surface energy than Aluminum
  Zn2+ instead of Na+ ions

## Slide 14: PVA-NaClO4 solid electrolyte

## Slide 15: PVA-ZnCl2 solid electrolyte

## Slide 16: XRD measurements